IIS

- Foreword

China Rare Earth Standardization Technical Committee (SAC/TC 229) is in charge of this English translation. In case of any doubt about the contents of English translation, the Chinese original should be considered authoritative.

This standard is drafted in accordance with the rules given in the GB/T 1.1—2020.

This standard was prepared by SAC/TC229.

Samarium-iron-nitrogen permanent magnetic powder for bonded magnet

# 1 Scope

This document specifies the classification and grade, requirements, test methods, inspection rules, packaging, marking, transportation, storage and accompanying documents of Samarium-iron-nitrogen(SmFeN) permanent magnetic powder for bonded magnet.

This document applies to isotropic and anisotropic SmFeN bonded permanent magnetic powders,which can be used in moulding, injection moulding, extrusion and calendering processes to produce bonded magnets.

# 2 Normative references

The following referenced documents are indispensable for the application of this document. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

GB/T 1479.1  Metallic powders—Determination of apparent density—Part 1：Funnal method

GB/T 9637  Electrotechnical terminology—Magnetic materials and components

GB/T 15676  Terms for rare earths

GB/T 19077  Particle size analysis—Laser diffraction methods

GB/T 24270  Method of measurement of temperature coefficient of magnetic properties of permanent magnetic materials

GB 39176  Rare earth products packing, marking,transport and storage

GB/T 40794  Measurement method of irreversible magnetic flux loss due to high temperature of rare earth permanent magnet

# 3 Terms and definitions

The following terms and definitions are applied to this document.

3.1

isotropic samarium iron nitrogen permanent magnetic powder

SmFeN permanent magnetic powder with the same magnetic properties when magnetised in any direction.

3.2

anisotropic samarium iron nitrogen permanent magnetic powder

SmFeN permanent magnet powders with magnetic properties much higher in one direction than in other directions.4 Classification and grades

# 4 Classification and grade

4.1 Classification

Permanent magnetic powders can be divided into two categories: isotropic and anisotropic.

4.2 Grade

Each product is divided into several grades according to the size of the maximum magnetic energy product and coercivity, see Table 1 for specific grades.

4.3 Designation

Designation of the grade of permanent magnetic powders are expressed by element symbols, product categories and technical parameters, as follows.：

SmFeN -X - ΧΧ/ΧΧ

Technical parameters (the mid-value of the maximum magnetic energy product and 1/10 of the lower limit value of the intrinsic coercivity)

The second level represents the product category, with the initial letter "I" of "isotropic" and the initial letter "A" of "anisotropic"

The first level represents the element symbol of the product, namely "SmFeN"

Note: For the convenience of distinguishing the grades, the first and second levels, the second and third levels are separated by the separator "-", and the maximum magnetic energy product and intrinsic coercivity of the third level product technical parameters are separated by the separator "/". The maximum magnetic energy product (BH) max is the mid-value of the specified upper and lower limits, and the intrinsic coercivity HcJ is 1/10 of the specified lower limit.

Example: SmFeN-I-127/72 indicates that the isotropic SmFeN permanent magnetic powder(BH) max is 119 kJ/m3~135 kJ/m3 (mid-value is 127 kJ/m3), HcJ is 717 kA/m~876 kA/m (lower limit value is 717 kA/m, taken 1/10 as 71.7, and rounded-up to 72).

# 5 Technical requirements

5.1 Main magnetic properties

The main magnetic properties of permanent magnetic powder at 20 ℃ shall meet the requirements of Table 1. If the demander has special requirements, the supplier and the demander can negotiate separately.. See Appendix A for the comparison table of the main magnetic properties of the International System of Units (SI) and the Electromagnetic System of Units (CGS), and the comparison table of the SI and CGS.

Table 1 The main magnetic properties of SmFeN permanent magnetic powder at 20 ℃

| Product | Main magnetic properties |
| --- | --- |
| Classification | Grade | Br T | HcJ kA/m | (BH)max kJ/m3 |
| Isotropic | SmFeN-I-80/56 | 0.65～0.70 | 557～717 | 72～88 |
|  | SmFeN-I-96/56 | 0.70～0.80 | 557～717 | 88～103 |
|  | SmFeN -I-104/64 | 0.80～0.85 | 637～796 | 96～111 |
|  | SmFeN -I-111/88 | 0.80～0.85 | 876～1035 | 103～119 |
|  | SmFeN-I-127/72 | 0.90～0.92 | 717～876 | 119～135 |
| Anisotropic | SmFeN -A-223/48 | 1.15～1.25 | 478～637 | 215～231 |
|  | SmFeN -A-239/56 | 1.15～1.25 | 557～717 | 231～247 |
|  | SmFeN -A-255/64 | 1.25～1.30 | 637～796 | 247～263 |
|  | SmFeN -A-271/64 | 1.30～1.35 | 637～796 | 263～279 |
|  | SmFeN-A-287/64 | 1.35～1.40 | 637～796 | 279～295 |
|  | SmFeN-A-303/80 | 1.40～1.50 | 796～955 | 295～310 |

5.2 Particle size

5.2.1 The D50 particle size of isotropic permanent magnetic powder is 50 μ m ~150  μ m. If the demander has special requirements, the supplier and the demander can negotiate separately.

5.2.2  The D50 particle size of anisotropic permanent magnetic powder is 1 μ m ~5  μ m. If the demander has special requirements, the supplier and the demander can negotiate separately.

5.3 Appearance quality

The isotropic permanent magnetic powder is silver gray, and the anisotropic permanent magnetic powder is black gray. The permanent magnetic particle shall be free of visible rust and inclusions.

5.4 Auxiliary magnetic properties and other physical properties

See Appendix B for auxiliary magnetic properties and other physical properties of permanent magnetic powder. If the demander has special requirements, the supplier and the demander can negotiate separately.

# 6 Test method

6.1 Main magnetic properties

The main magnetic properties of permanent magnetic powder shall be tested with a vibrating sample magnetometer meeting the accuracy requirements. The detection method of isotropic permanent magnet powder refers to Appendix D of GB/T 20168-2017, and the detection method of anisotropic permanent magnet powder refers to Appendix D of GB/T 41967-2022.

6.2 Particle size

The particle size test method of permanent magnetic powder shall be carried out according to the GB/T 19077.

6.3 Appearance quality

Visual inspection is recommended for the detection of the appearance of permanent magnetic powder. If the demander has special requirements, the supplier and the demander can negotiate separately.

6.4 Auxiliary magnetic properties and other physical properties

6.4.1 The measurement of magnetic property temperature coefficient of permanent magnetic powder and magnet prepared by permanent magnetic powder shall be measured according to the GB/T 24270.

6.4.2 The maximum working temperature of the magnet prepared by permanent magnetic powder shall be measured according to the GB/T 40794.

6.4.3 The loose density of permanent magnetic powder shall be measured according to the GB/T 1479.1.

# 7 Inspection rules

7.1 Inspection and acceptance

7.1.1 The products shall be subject to factory inspection by the supplier or a third party, and the quality shall comply with the provisions of this document.

7.1.2 The Demander shall inspect the received products according to the provisions of this document. If the inspection results are inconsistent with the provisions of this document, a written explanation shall be provided to the supplier within 1 month from the date of receipt of the product, and the supplier and the supplier shall negotiate for settlement.

7.2 Batching

The same batch of products shall be of the same brand.

7.3 Inspection items

The main magnetic properties, grain size and appearance of each batch of products shall be inspected before delivery.

7.4 Sampling

The number of samples (bags) for each batch of products shall be in accordance with Table 2. Each sample is 50 g, and the sample shall be sealed and packaged. The sampling method is sampling.

Table 2 Sampling Program

| Pieces per batch | 1 | 2～10 | 11～60 | 61～100 | 101～150 | > 150 |
| --- | --- | --- | --- | --- | --- | --- |
| Number of sampling pieces | 1 | 2 | 3 | 4 | 5 | 6 |

7.5 Judgment rules

7.5.1 Main magnetic properties

When the main magnetic properties of permanent magnetic powder test results failed, double samples should be taken from the batch of permanent magnetic powder to repeat the test on the failed items, if the test results are qualified, the batch of permanent magnetic powder is judged to be qualified; if the results are still unqualified, the batch of permanent magnetic powder is judged to be unqualified.

7.5.2 Particle size

If the particle size of the permanent magnetic powder fails to pass the test, the batch of permanent magnetic powder is judged to be unqualified. If the demander has special requirements, both the supplier and the demander can agree separately.

7.5.3 Appearance Quality

The batch of permanent magnetic powder is judged to be unqualified if the inspection result of the appearance quality of the permanent magnetic powder is not qualified.

# 8 Packaging, marking, transportation, storage and accompanying documents

8.1 Packaging, marking, transportation and storage

Product packaging, marking, transportation and storage should be carried out in accordance with the provisions of GB 39176.

8.2 Accompanying documents

Each batch of products should be accompanied by accompanying documents, including but not limited to

a) Product Certificate of Conformity (including supplier information, product information, document number, factory date or packaging date).

b) Certificate of quality (including manufacturer's name, product name, grade, lot number, net weight and number of pieces, file number, factory or packaging date).

c) the main magnetic properties and particle size inspection report.

d) instructions for use of the product.

Appendix A

Comparison table of the main magnetic properties of SmFeN permanent magnet powder in SI and CGS

The comparison table of the main magnetic properties of permanent magnetic powder in the International System of Units (SI) and the Electromagnetic System of Units (CGS) at 20℃ is shown in A.1.

Table A.1 Comparison table of main magnetic properties of samarium iron and nitrogen permanent magnet powder

| Materials | Main magnetic properties |
| --- | --- |
| Grade | SI | CGS | Br | HcJ | （BH）max |
|  |  |  | T | kGs | kA/m | kOe | kJ/m3 | MGOe |
| Isotropic | SmFeN-I-80/56 | SFN-I-1008 | 0.65～0.70 | 6.50～7.00 | 557～717 | 7.00～9.00 | 72～88 | 9.00～11.00 |
|  | SmFeN-I-96/56 | SFN-I-1208 | 0.70～0.80 | 7.00～8.00 | 557～717 | 7.00～9.00 | 88～103 | 11.00～13.00 |
|  | SmFeN-I-104/64 | SFN-I-1309 | 0.80～0.85 | 8.00～8.50 | 637～796 | 8.00～10.00 | 96～111 | 12.00～14.00 |
|  | SmFeN-I-111/88 | SFN-I-1412 | 0.80～0.85 | 8.00～8.50 | 876～1035 | 11.00～13.00 | 103～119 | 13.00～15.00 |
|  | SmFeN-I-127/72 | SFN-I-1610 | 0.90～0.92 | 9.00～9.20 | 717～876 | 9.00～11.00 | 119～135 | 15.00～17.00 |
| Anisotropy | SmFeN -A-223/48 | SFN-A-2807 | 1.15～1.25 | 11.50～12.50 | 478～637 | 6.00～8.00 | 215～231 | 27.00～29.00 |
|  | SmFeN -A-239/56 | SFN-A-3008 | 1.15～1.25 | 11.50～12.50 | 557～717 | 7.00～9.00 | 231～247 | 29.00～31.00 |
|  | SmFeN -A-255/64 | SFN-A-3209 | 1.25～1.30 | 12.50～13.00 | 637～796 | 8.00～10.00 | 247～263 | 31.00～33.00 |

| Materials | Main magnetic properties |
| --- | --- |
| Grade | SI | CGS | Br | HcJ | （BH）max |
|  |  |  | T | kGs | kA/m | kOe | kJ/m3 | MGOe |
|  | SmFeN -A-271/64 | SFN-A-3409 | 1.30～1.35 | 13.00～13.50 | 637～796 | 8.00～10.00 | 263～279 | 33.00～35.00 |
|  | SmFeN-A-287/64 | SFN-A-3610 | 1.35～1.40 | 13.50～14.00 | 637～796 | 8.00～10.00 | 279～295 | 35.00～37.00 |
|  | SmFeN-A-303/80 | SFN-A-3810 | 1.40～1.50 | 14.00～15.00 | 796～955 | 10.00～12.00 | 295～310 | 37.00～39.00 |
| Note: The conversion relationship between the International System of Units (SI) and the Electromagnetic System of Units (CGS) is: 1 T＝10 kGs；1 kA/m ＝4π× 10-3 kOe；1 kJ/m3＝4π×10-3 MGOe。 |

Appendix B

Auxiliary magnetic properties and other physical properties of SmFeN permanent magnetic powders

The auxiliary magnetic properties and other physical properties of permanent magnet powders are shown in Table B.1.

Table B.1 Auxiliary magnetic properties and other physical properties of samarium-iron-nitrogen permanent magnetic powder

| Performance Items | Unit | Performance Index |
| --- | --- | --- |
| Temperature coefficient of residual magnetic inductionα（Br） | %/(C | －0.15 ~ －0.06 |
| Temperature coefficient of intrinsic coercivityβ（HcJ） | %/(C | －0.60 ~－0.40 |
| Curie temperatureTc | (C | 350 ~ 500 |
| Maximum operating temperatureTw (For cylindrical magnets with L/D=0.7, irreversible loss=5% of the maximum holding temperature at a constant temperature of 2 hours) | (C | 80 ~ 200 |
| Loose packing density | g/cm3 | 2.00 ~ 3.50 |
| Theoretical densitiesρ | g/cm3 | 7.40 ~ 7.75 |
| Note: The temperature range for α (Br) and β (HcJ) measurements is 20 C~ 100 C, but it does not indicate that the permanent magnet powder can only be used in this temperature range. |

# Text boxes

Samarium-iron-nitrogen permanent magnetic powder for bonded magnet

钐铁氮粘结永磁粉

（English Translation）

20XX-XX-XX发布                                      20XX-XX-XX实施

GB/T XXXXX—20XX

B

ICS 77.120.99

CCS H 65

Issued by  General Administration of Quality Supervision, Inspection and

Quarantine of the People's Republic of China

Standardization Administration of the People's Republic of China

Implementation date: 202X-XX-XX

Issue date: 202X-XX-XX发布

National Standard of the People's Republic of China